## Slide 1
A lightening fast survey of various glass technology bits and pieces

## Slide 2
Typical Corning Glass Batch Sheet for Experimental Glass Melt: The heart of the original glass business

## Slide 3
9 (nine) Crucible gas fired melt furnace, Sullivan Park Labs CGW
Melting Technology Technicians quenching a melt

## Slide 4
Glass Composition Phase Diagram
Underlying crystalline habits that characterize the various glass formation regions vs. quench rate
Slow quench rate
(smallest field of glass formed)
modest quench rate
(medium field of glass formed)
fast quench rate
(largest field of glass formed)

## Slide 5
Taken from CGW Survey Manual of CGW product glass (D. Thompson, 1985)

## Slide 6
Effect of soft lithia glass in silica matrix after HF etch
X22,400 (SEM)
Examples of bi-phasic glass; example 1:Vycor
Called “Sticky glass”
…can embed/bind chemicals to surface

## Slide 7
Examples of bi-phasic glass; example 2
Pyrex (>50,000X)
(silver ions have been `intercalated’ into structure
to reveal biphasic character)
Pyrex is a combination of `softer’ glass (so it flows under flame )and a much harder glass (so it resists chemical and physical change)

## Slide 8: Scanning Electron Microscopy (SEM)
Optical Microscopy
(obs) ~ 500 nm ~minimum object size
1000X practical maximum magnification
A. Leeuwenhoek 1632-1723

## Slide 9
Electron microscopy: a breakthrough microscopy
=h/p (De Broglie equation) ~ 0.002 nm for 300 keV beam (minimum theoretical limit)
Practically=>Can see 0.1-1 nm objects
higher beam energy, lower 
40-100,000 X magnifications
Manfred v. Ardenne 1907-1997
invents in 1937
Charles Oakley
1904-1996
develops in 1947

## Slide 10: BASICS of SEM technique
Main imaging methods
Secondary electrons (SE)
Backscattered electrons (BSE)
Main analytical method
XRED = EDX (same)
(X-Ray Energy Dispersion or Energy Dispersive analysis of X-rays
1-10 keV
Beam spot typically 0.2 nm)

## Slide 11: Some Geeky Details Of SEM
Auger (pronounced OJay)=surface state electrons
Inelastic BSE =impacting electrons re-scattered (sensitive to atomic masses producing scattering)
SE = electrons re-emitted by absorbing materials (provides great depth of field & primary image)
Characteristic x-rays= energy spacings of elements (used for XRED=EDX)
Electron beam produces a characteristic tear-drop shaped hole in material, which vomits electrons and x-rays
5-100 um
0.2-2 nm spot

## Slide 12: More geeky details of SEM:SE detection

## Slide 13: Typical `SE’ images
Cheese at 1500X
Spider mite
Hair on spider mite’s leg
Ballatidium coli (stomach protozoan) at ~5000X

## Slide 14: Yet more geeky details: BSE & EDX
Magnetic doughnut used to gather BSE and direct into SE (Everhart-Thornley) detector
BSE electrons
BSE provides map of element and compound distributions
(but poor depth of field)
BSE=backscattered electrons

## Slide 15
Basic SEM
XRED (x-ray energy dispersion unit)…an add-on unit
SEM and accompanying XRED spectrum of scanned region
Elemental analysis EDX
Sampling Limitation
Sample volume and area depend on beam
Top not like insides ?

## Slide 16: The last few details on SEM
Metals and other conductors can be observed without preparation
Non-conductors (glasses, ceramics, biological and organic samples) need to be coated with a conductive thin layer or the beam will cause local `melt’ down at beam focus and sample will glow
+ -
Au or C
Evacuated chamber
Filament power
Coated sample
Schematic of an SEM coater
Initially uncoated sample

## Slide 17: DSC (Differential Scanning Calorimetry)*
Schematic of basic DSC/DTA
Thermocouple pair (measures T difference)
Heated strip
(can go to 1800 C)
DSC if heat difference measured;
DTA (differential temperature analysis if temperature difference measured)
measures exo or endothermic (sample-reference) response vs input energy (or temperature) of strip
Power supply/interface

## Slide 18: Glass transition (Tg) and crystallization (Tc) (=devitrification)
Tg Tc
Glass melt is quenched faster than structure can reorganize into crystallographically ordered arrays=> quenched glass has no thermodynamic definition…glass is not a liquid (which is defined)
Disorder is a function of quench rate
Supercooled liquid is semi-ordered and thermodynamically defined
It takes energy to `reorganize’ chaos into supercooled order=> why Tg is endo proces
T
Q(cal)
‘supercooled liquid structure’
Disordered glass
Ordered crystal structure
Tg
Tc

## Slide 19: Kinds of thermograms
Single phase, melting
(e.g. cubic NaCl)
Crystal-crystal transition followed by melting (tridymite silica->cristobalite silica)
Release of hydration water (e.g CuSO4*5H2O)
Simple glass thermogram
(e.g. glassy silica->cristobalite)
mp (endo)
Phase change (exo)
Melting
Dehydration (exo)
melting

## Slide 20
Some useful facts to help sort out DSC curves
1) Typical melting points for selected materials
MATERIAL MELTING POINT, O C
Pyrex glass 1250
Soda lime glass 1000-1050
Most inorganic salts 600-900
(NaCl, CaCl2, KCl)
Plastics <400
Silica (glass or crystal) ~1800

## Slide 21
More useful facts to help sort out DSC curves
2) Glass transition temperatures (Tg) for selected glassy materials
Glass Tg O C
Silica (glass) ~1200
Pyrex glass 550
Soda-lime glass (crap) 500- 550
Plastics < 100

## Slide 22
And yet more useful facts to sort out DSC curves
1) Waters of hydration make multiple sharp, (weak) exothermic peaks
2) crystal-crystal transitions (Tcc) make pretty sharp, (strong) exothermic peaks
3) glass-crystal transitions (Tgc) make broad, (strong) exothermic peaks
4) For a glass, Tg < Tgc < Tcc

## Slide 23: XRD (X-ray Diffraction)
Basic `X-ray powder diffraction’ camera (Debye-Scherrer design)
Bragg’s Law: 2*d*sin=
Given fixed  & a measure of the angle , you can determine atomic spacing d
The key point….
X-rays in
X-rays in
Diffracted X-rays
Diffraction pattern of DNA
Taken by Rosalind Franklin

## Slide 24: Details of Debye-Scherrer XRD diffraction camera
rings
or
lines

## Slide 25
Typical powder x-ray diffractometer instrument
X-ray source
(Cu-K 1.54 A=0.15 nm)
Detector camera in here
Powdered sample mounted (and turned) in here

## Slide 26: Examples of XRD spectra
Pure crystalline substance
Glass only (`glass halo’)
Partially `devitrified’ glass*
Only lines…all crystal
Halo + lines= glass + crystal (devitrified glass)
Halo only= all glass

## Slide 27
We is done with the glass sh*t
(almost…)